## Slide 1: Nanoparticle Formation and Deposition during Combustion of Iron Microparticles using Euler-Lagrange Simulations
David Märker1 Nils Hartmann2 Tien Duc Luu1 Andreas Kronenburg2 Oliver T. Stein1
1 Engler-Bunte-Institute, Simulation of Reacting Thermo-Fluid Systems, Karlsruhe Institute of Technology
2 Institute for Reactive Flows, University of Stuttgart
,
,
,
,

## Slide 2: Metal enabled cycle of renewable energies (MeCRE)
[1]
[1] Hasse, C., et al. (2025) https://www.tu-darmstadt.de/clean-circles/about_cc/index.de.jsp; [2] Chang, D., et al. (2025) Fuel 397: 135366; [3] Buchheiser, S., et al. (2023) Materials 16(5): 2009.
[2]
[2]
[3]
Nanoparticle Deposition
[2]

## Slide 3: Modelling: Microparticle Oxidation and Nanoparticle Formation
Fe
Fe(g)
Fe
FeO
Fe
FeO
O2
Evaporation
Nanoparticle Transport
Advection
Mass Diffusion
Thermophoresis
[4] Mich, J., et al. (2023) Combustion and Flame 256: 112949 [5] Nguyen, B.-D., et al. (2025) Chemical Engineering Journal 507: 160039
Inception
Fe(g)
O2
FeO(g)
NP
Nanoparticle Formation
Oxidation
Growth
Collison rate approach

## Slide 4: Simulation Approaches
Boundary Layer Resolved
Euler-Lagrange
Evaporation Model
Nanoparticle Formation Model
Deposition Model
Oxidation Model
Goal: Make use of the BLRS results to develop models for the unresolved boundary layer in EL
Evaporation Model
Nanoparticle Formation Model
Deposition Model
Oxidation Model
Requires multiple models Computationally Efficient More versatile in terms of scalability
Precise calculations Computationally expensive Limited scalability

## Slide 5: Boundary Layer Resolved Simulation
Video BLRS Multiparticle
Hot Air (1800 K, 0.5 m/s)
Euler-Lagrange Cell Size

## Slide 6: Modelling Boundary Layer Processes: Evaporation and Nanoparticle Formation
Fe
FeO
Boundary Layer Resolved
Euler-Lagrange
Cell values are known, surface values require modelling
?
✓
Evaporation
Iron concentration gradient?
           Sherwood correlation
Values of ?
 Film values with 1/3-rule
Nanoparticle Formation
Happens close to the particle surface
Effect of heat release in the boundary layer?

## Slide 7: Modelling Boundary Layer Processes: Evaporation and Nanoparticle Formation
Fe
FeO
Remaining quantities?
Surface values
Thermophoretic velocity
Nanoparticle volume fraction
Impose BLRS data for EL sub-models

## Slide 8: Comparison: Evaporation Rates from BLRS & EL
Evaporation rates are nicely matched as long as the microparticle temperature is pre-set

## Slide 9: Comparison: Evaporation Rates from BLRS & EL Effect of the Nanoparticle Formation Model
includes and .
One-step approach
Collision rate as in BLRS
The single-step condensation and oxidation model better matches the BLRS results.

## Slide 10: Open Challenges
  How to obtain the nanoparticle volume fraction at the surface?
Fe
FeO
Oxygen Consumption
Iron Evaporation
Stefan Flow
How are mass and heat transport affected?
  Do existing Nusselt and Sherwood correlations still work?
Nanoparticle Formation
How to model the nanoparticle deposition?
Surface Velocity from Stefan Flow
Thermophoretic Velocity possibly via the Nusselt Number
Fe
FeO

## Slide 11
We gratefully acknowledge the funding by the Friedrich-and-Elisabeth-Boysen Foundation under grant number BOY-195. We thank Bich-Diep Nguyen, Arne Scholtissek, and Christian Hasse (TU Darmstadt) for their support during development of the BLRS solver through the Clean Circles Project.

## Slide 12: Appendix

## Slide 13: Governing Equations in the Eulerian Phases

## Slide 14: Particle Temperature in EL

## Slide 15: Comparison to experimental results
Experimental Images: Li, T., et al. (2026) Fuel 404: 136303.

## Slide 16: Extension to multiple particles

## Slide 17: Nanoparticle Formation: Evaporation Path
Microparticle
Fe
FexOy
O2
Evaporation
Fe(g)
Homogeneous Nucleation
Condensation
Coalescence
Oxidation
FexOy Nanodroplets
Phase Transition
Nanoparticles
Agglomeration
Fe Nanodroplets
Deposition

## Slide 18: Nanoparticle Formation: Possible pathways
Fe(g)
Fe
FexOy
O2
Evaporation
Nanoparticle Formation by Condensation
Oxidation, Phase Transition and Agglomeration
O2
Nano Fragmentation
Microexplosions
Evaporation Path
Microexplosion Path

## Slide 19: Setup and models
Combustion kinetics: First order surface kinetics (FOSK)
Kinetically limited:
Diffusion limited:
[S1] Mich, J., et al. (2023) Combustion and Flame 256: 112949 [S2] Nguyen, B.-D., et al. (2025) Chemical Engineering Journal 507: 160039
Stefan Flow
Thermophoresis

## Slide 20: Energy density and specific energy
Bergthorson, J., et al. (2015) Applied Energy 160: 368-382

## Slide 21: Metal fuels – An energy carrier in a global system
For Reference: 50 L Diesel (36 MJ/L)  ≈ 1000 km
100 km
LH2: 8,5 MJ/L  236 km
LNG: 22 MJ/L  610 km
Iron: 58 MJ/L  1610 km
Sadeghinezhad, E., et al. (2013) Renewable and Sustainable Energy Reviews 28: 410-424; Alkhaledi, A. N., et al. (2022) Ships and Offshore Structures 17(7): 1555-1564; Boretti, A. (2020) Applied Sciences 10; Fischer, S. H. and Grubelich, M. (1998) Sandia National Lab.(SNL-NM), Albuquerque, NM.

## Slide 22: Burning modes
Bergthorson, J., et al. (2015) Applied Energy 160: 368-382

## Slide 23: Phase diagram
Thijs, L.C., et al. (2025) Combustion and Flame 271: 11382

## Slide 24: Temporal temperature development: array
dp = 36 µm

## Slide 25: Boundary Layer Resolved Simulation
Video BLRS Multiparticle
Hot Air
(1800 K, 0.5 m/s)
Euler-Lagrange Cell Size

## Slide 26: Modelling: Microparticle Oxidation and Nanoparticle Formation
Fe
Fe(g)
Fe
FeO
Fe
FeO
O2
Evaporation
Nanoparticle Formation
Nanoparticle Transport
Inception:
Growth & Oxidation:
Advection
Mass Diffusion
Thermophoresis
[4] Mich, J., et al. (2023) Combustion and Flame 256: 112949 [5] Nguyen, B.-D., et al. (2025) Chemical Engineering Journal 507: 160039

## Slide 27: Modelling Boundary Layer Processes: Evaporation and Nanoparticle Formation
Fe
FeO
Boundary Layer Resolved
Euler-Lagrange
Cell values are known, surface values require modelling
?
✓
Evaporation
Iron concentration gradient?
           Sherwood correlation
Values of ?
 Film values with 1/3-rule
Nanoparticle Formation
Primarily happens close to the particle surface
Effect of heat release from condensation and oxidation in the boundary layer?

## Slide 28: Open Challenges
How are mass and heat transport affected by
  Nanoparticle formation in the BL
  Co-flowing iron and oxygen streams in the BL (especially at high ambient temperatures)
  Do existing Nusselt and Sherwood correlations still work?
How to model the deposition of nanoparticles
  Stefan velocity at the surface ✓
  Thermophoretic velocity possibly obtainable from Nusselt number
  Nanoparticle volume fraction at microparticle surface
Fe
FeO
Oxygen Consumption
Iron Evaporation
Stefan flow